## Slide 1
This network is EPSRC Funded under Grant No: EP/S000356/1
AI4SD Hackathon
Defect detection in Graphene Sheets
Group 5. Anna Bachs Herrera, Abdoulatif Cisse, Emilio Alexis de la Cruz Nuñez Andrade, Philipp Deussen, Ivan Yankov

## Slide 2: Index
Introduction
Workflow
Results
Conclusions & Future Work
AI4SD Hackathon

## Slide 3: Introduction
Classification:
  Defect
  No defect
AI4SD Hackathon
180 micrographs
256x256
Perfect patches
2279 patches
48x48
Defect patches
32 patches
48x48

## Slide 4: Workflow
AI4SD Hackathon
Perfect: 2279
Defect: 32
Perfect: 2000
Defect: 2000

## Slide 5: Workflow
AI4SD Hackathon

## Slide 6: Workflow
AI4SD Hackathon
Validation Set
Training Set

## Slide 7: Workflow - Results
AI4SD Hackathon

## Slide 8: Other attempt: PCA model for image analysis
AI4SD Hackathon
Display Graphene images
Identify principal component
  Edge detection
  RGB density
To visualise: 2 PC’s
Eigenvalue Problem:
max ()

## Slide 9: PCA model for image analysis
AI4SD Hackathon
4. Train model on ca. 2000 perfect Graphene images
5. Pre-process across the number of batches (images)

## Slide 10: PCA model for image analysis
AI4SD Hackathon
5. Test new images against the correct PCA shape
6. Differences in scores reflect a difference of images
Trained shape (correct) | Defected shape

## Slide 11: Conclusions & Future Work
Small dataset
Relevant features extracted
AI4SD Hackathon